# Text boxes

TECHNICAL DATA SHEET

USC Aerosol Under Coating

TECHNICAL CALLS: 1-855-746-4872 (1-855-RING USC)

DESCRIPTION:  USC Under Coating is An autobody undercoating for application to the undercarriage for rust protection and sound deadening. Asphalt base undercoating remains pliable and resists temperature extremes. Sprays evenly and dries completely to a smooth consistency. Does not sag and dries quickly.

PART NUMBER:  51333

PRODUCT USES:

Panel & fender undersides

Hoods & decks

Trunk interiors

Section repairs

Weld joints

Rust holes

All chassis parts

Packaging:

UPC Code                              037307513339

Cans per case                        12

Shipping weight per case        19.6 lbs.

Container                              20 fluid ounce can

Label weight                          18 ounces (511 grams)

Shipping Classification             Consumer Commodity

ORM-D UN 1950

Hazard Class                    2.1

Properties:

Flammability                 “Extremely Flammable”

Flash point                    -4o F

Specific Gravity             0.80

Solids Content              ~40%

VOC content                  ~29%, cannot exceed 40%

MIR value                      ~0.30

HAPs content                 4%

Storage Temperature     40-90F

Application Temperature 50-100F

Durability                        Very Good

Abrasion Resistance      Very Good

Heat Resistance             300o F

Gasoline Resistance       No

Resin System                  Petroleum Asphalt

Shelf life                           Guaranteed for 2 years

Dry Time*:

To touch                                   10 minutes

To handle                                  6 hours

*At 720 F, 50% humidity,

1.5 mil thickness

**Curing/Recoat time is extended with

multiple coats and excessively thick

coats**

Gloss*:                                      Low Lustre, 15-25

*as measured on a 600 gloss meter

U.S. Chemical & Plastics ● A Valspar Company • 600 Nova Dr. SE ● Massillon, Ohio  44646

USChem.com                                                                                    Phone: 330-830-6000

Form: TDSUSC51333  01/16